## Slide 1: Nonlinear Cavity Response under Coherent Excitation: Numerical and Experimental Investigation
Samuel Serna1,2
Jeremy Oden1, Xavier Le Roux2, Philippe Delaye1, Eric Cassan2,
Nicolas Dubreuil1
1Laboratoire Charles Fabry, Institut d'Optique Graduate School, Université Paris-Saclay, CNRS, France
2Institut d’Électronique Fondamentale, Univ. Paris-Sud, UMR 8622, Université Paris-Saclay, CNRS, France

## Slide 2: PhC Microcavities in Semi-Conductors
Strong light confinement
High density of energy stored in microcavities
Figure of Merit = Q/V
2

## Slide 3: Nonlinear Optical Microcavities
All-optical switches in PhC semiconductor microcavities
E. Weidner, et al. Applied Physics Letters, 90, (2007), S. Combrié, et al. Opt. Lett., 33, 1908 (2008), C. Husko, et al. Appl. Phys. Lett., 94, 021111 (2009)
Silicon :
GaAs :
Tanabe et al., App. Phys. Lett 87 151112 (2005)
InGaAsP :
Nozaki et al., Nat. Photon. 4, 248 (2012)
All-optical switching with pump energy of 10 fJ !
GaInP :
V. Eckhouse et al., Opt. Express 20, 8524 (2012)
InP :
F. Raineri et al., App. Phys. Lett 85, 1880 (2004)
3

## Slide 4: Nonlinear Optical Microcavities
All-optical switches in PhC semiconductor microcavities
Transmission
Frequency
1 µm
Signal
&
Control
GaAs Microcavity
Generation of free-carriers
 Frequency blue-shift
C. Husko, Appl. Phys. Lett. 94, 021111 (2009)
4

## Slide 5: Nonlinear Optical Microcavities
All-optical switches in PhC semiconductor microcavities
1 µm
Signal
&
Control
GaAs Microcavity
Generation of free-carriers
 Frequency blue-shift
C. Husko, Appl. Phys. Lett. 94, 021111 (2009)
Transmission
Frequency
4

## Slide 6: Nonlinear Optical Microcavities
All-optical switches in PhC semiconductor microcavities
1 µm
Signal
&
Control
GaAs Microcavity
Generation of free-carriers
 Frequency blue-shift
C. Husko, Appl. Phys. Lett. 94, 021111 (2009)
Transmission
Frequency
Frequency detuning issues :
limitation in the coupling efficiency of the control pulse
Cavity enhancement effect is not maintained for the entire pulse duration
Ringing behavior : leads to a temporal distorsion of the pulse
Time
Power (a.u.)
4
Notes: Whereas the nonlinear refractive index change induced by the pulse front edge detunes the cavity resonance, it also contributes to a decrease of the coupling efﬁciency for the rest of the pulse. It means that only one part of the pulse energy is effective to perform the optical switching operation.

## Slide 7
Nonlinear Optical Microcavities
QUESTION :
Is there a way to control the light-localization effect in a nonlinear optical resonator ?
ISSUES to be addressed
More efficient way to excite a cavity in nonlinear regime ?
Enhancement of the intra-cavity light-matter interaction ?
Any control on the NL freq. shift ΔωNL + intra-cavity fields dynamics ?
5

## Slide 8
Nonlinear Optical Microcavities
QUESTION :
Is there a way to control the light-localization effect in a nonlinear optical resonator ?
ISSUES to be addressed
More efficient way to excite a cavity in nonlinear regime ?
Enhancement of the intra-cavity light-matter interaction ?
Any control on the NL freq. shift ΔωNL + intra-cavity fields dynamics ?
 Coherent excitation of atomic and molecular resonances
D. Meshulach, Nature 396, 239 (1998)
B. Chatel & B. Girard, in Femtosecond Laser Spectroscopy, Springer (2005)
5

## Slide 9
Input pulse
Intracavity pulse
S. Sandhu et al., App. Phys. Lett. 96, 231108 (2010)
6
Coherent Control & Opt. Resonator

## Slide 10
Input pulse
Intracavity pulse
Spectral phase = dispersion shape of the optical resonance
Enhancement of the intracavity peak energy
Application : bistable operation with reduced control power + phase switching operation
P. T. Kristensen et al. App. Phys. Lett. 102, 041107 (2013)
6
S. Sandhu et al., App. Phys. Lett. 96, 231108 (2010)
Coherent Control & Opt. Resonator

## Slide 11
J. Oden et al., J. Europ. Opt. Soc. Rap. Public. 8, 13046 (2013)
Silicon Microcavity
7
Coh. Excitation of a NL Microcavity

## Slide 12
Refractive index variation
Nonlinear losses
Two-photon absorption (TPA)
Free carrier absorption (FCA)
Transmission
Frequency blue-shift
Optical Kerr eﬀect
Free carrier refraction (FCR)
7
J. Oden et al., J. Europ. Opt. Soc. Rap. Public. 8, 13046 (2013)
Silicon Microcavity
Coh. Excitation of a NL Microcavity

## Slide 13
 Linear time variation of the cavity resonance
7
Refractive index variation
Nonlinear losses
Two-photon absorption (TPA)
Free carrier absorption (FCA)
Transmission
Frequency blue-shift
Optical Kerr eﬀect
Free carrier refraction (FCR)
J. Oden et al., J. Europ. Opt. Soc. Rap. Public. 8, 13046 (2013)
Silicon Microcavity
Coh. Excitation of a NL Microcavity
Notes: accurately tailored chirped pulse, whose instantaneous frequency coincides with the nonlinear resonance drift, which allows the light to efﬁciently build-up inside the cavity

## Slide 14
Q=5260  τcav=4.4 ps
Vcav = 0.8(λ/n)3
P. Velha et al., Appl. Phys. Lett. 89, 171121 (2006).
Δω0
Design: Fabry-Perot type cavity with two-tapered Bragg mirrors
Fabrication: Minerve @ IEF – Univ. Paris-Sud
Silicon Microcavity
1 µm
7
Coh. Excitation of a NL Microcavity

## Slide 15
ω
Time
Time
 Coherent excitation using a chirped pulse
P. Velha et al., Appl. Phys. Lett. 89, 171121 (2006).
Design: Fabry-Perot type cavity with two-tapered Bragg mirrors
Fabrication: Minerve @ IEF – Univ. Paris-Sud
Silicon Microcavity
7
Coh. Excitation of a NL Microcavity

## Slide 16
 Coherent excitation using a chirped pulse
P. Velha et al., Appl. Phys. Lett. 89, 171121 (2006).
Design: Fabry-Perot type cavity with two-tapered Bragg mirrors
Fabrication: Minerve @ IEF – Univ. Paris-Sud
Silicon Microcavity
7
Coh. Excitation of a NL Microcavity
ω
Time
Time
α

## Slide 17
ω
Time
Time
 Coherent excitation using a chirped pulse
α
Dispersion Coefficient
Absorbed Energy
P. Velha et al., Appl. Phys. Lett. 89, 171121 (2006).
Design: Fabry-Perot type cavity with two-tapered Bragg mirrors
Fabrication: Minerve @ IEF – Univ. Paris-Sud
Silicon Microcavity
7
Coh. Excitation of a NL Microcavity

## Slide 18
 Coherent excitation using a chirped pulse
Silicon Microcavity
7
Coh. Excitation of a NL Microcavity

## Slide 19
150 fs pulses
@ 50 MHz
Grating-based pulse stretcher
O.E. Martinez, IEEE JQE 23, 59 (1987)
8
Coherent Excitation Set-up

## Slide 20
150 fs pulses
@ 50 MHz
8
Coherent Excitation Set-up
Grating-based pulse stretcher
O.E. Martinez, IEEE JQE 23, 59 (1987)
Pulse shaper

## Slide 21
Wavelength [nm]
Power [a.u.]
8
Coherent Excitation Set-up
150 fs pulses
@ 50 MHz
Grating-based pulse stretcher
O.E. Martinez, IEEE JQE 23, 59 (1987)

## Slide 22
Transmission spectra with chirp varying from ϕ(2)= -3.5 to +3.5 ps2.
9
Uincident= 3 pJ = Cste
Coh. Excitation : Exp. Demonstration

## Slide 23
Transmission spectra with chirp varying from ϕ(2)= -3.5 to +3.5 ps2.
ϕ(2)=+1.6 ps2
Equal Pulse duration
5.7 ps (Autocorr = 8 ps)
ϕ(2)=-1.6 ps2
9
Uincident= 3 pJ = Cste
First exp. demonstration :
Coherent Excitation of a NL µcavity
Coh. Excitation : Exp. Demonstration
ϕ(2)=0 ps2

## Slide 24
10
Coh. Excitation : Num. Model
 | (1)
 | (2)
 | (1)
 | (2)
 | Value
 | Value
Paul Barclay et. al,
Opt. Express 13, 801-820 (2005)

## Slide 25
 | (1)
 | (2)
 | (1)
 | (2)
10
Coh. Excitation : Num. Model
Paul Barclay et. al,
Opt. Express 13, 801-820 (2005)
Effect of 2.5 mm
waveguide
4.5 W injected
 | Value
 | Value

## Slide 26
Transmission spectra with chirp varying from ϕ(2)= -3.0 to +3.0 ps2.
Nonlinear Frequency shift
Carrier Density
× 2
10
First exp. demonstration :
Coherent Excitation of a NL µcavity
Enhanced nonlinear interaction
Uincident= 3 pJ = Cste
Coh. Excitation
Equal Pulse duration
5.7 ps (Autocorr = 8 ps)
nW

## Slide 27
Transmission spectra with chirp varying from ϕ(2)= -3.0 to +3.0 ps2.
10
First exp. demonstration :
Coherent Excitation of a NL µcavity
Enhanced nonlinear interaction
Uincident= 3 pJ = Cste
Coh. Excitation
nW
a.u.
Simulation

## Slide 28
By controling the linear chirp  COHERENT EXCITATION
Nonlinear interaction enhancement
First Experimental Demonstration of the Coherent Excitation of a NL Opt. Resonator
ωcav.
Experiment
Simulations
Free carrier density x 2
Cavity Bandwidth x 20
11
time
Capability to manipulate the optical bandwidth & the nonlinear dynamics of a cavity
Conclusion

## Slide 29
More complex pulse shaping (Amplitude & Phase) using SLM based pulse shaper
Deeper exploitation of the model
Experimental study of the nonlinear cavity dynamics
Application for :
  ACTIVE microcavities
  Coupled resonators
12
Perspectives
Acknowledgements
Scholarship from the Ministry of Higher Education and Research (France).

## Slide 30
(x12)
INPUT PULSE = Fourier-Limit pulse (ϕ(2)=0)
ΔλP = 5.7 nm (≈20×Δλ0 )  τcorr=2 ps
Injected Energy = 3 pJ
9
NL Cavity Transmission

## Slide 31
(x12)
INPUT PULSE = Fourier-Limit pulse (ϕ(2)=0)
ΔλP = 5.7 nm (≈20×Δλ0 )  τcorr=2 ps
Injected Energy = 3 pJ
blue-shift of the cavity resonance : ΔλNL = 1.4 nm
9
NL Cavity Transmission

## Slide 32
ϕ(2)=0 ps2
Transmission spectra with chirp varying from ϕ(2)= -3.5 to +3.5 ps2.
ϕ(2)=+1.6 ps2
Equal Pulse duration
5.7 ps (Autocorr = 8 ps)
ϕ(2)=-1.6 ps2
10
Uincident= 3 pJ = Cste
First exp. demonstration :
Coherent Excitation of a NL µcavity
Coh. Excitation

## Slide 33
0.4 pJ.
Δωp = 30 ω/Q
φ(2)= τp /Δωp = Q2/(30 ω2)=+1.3 ps2